**SCREEING REPORT**

**Test Number:** 14462C00  **Date:**2020-02-14

**Sample Name:** Renata CR2032REN

**Chemistry:** Li/MnO2

**Voltage Statistic Table**

All samples OCV CCV

**Maximum:** **3.282** **3.214**

**Minimum:** **3.255** **3.018**

**Median:** **3.274** **3.200**

**Mean (M):** **3.274** **3.193**

**Stander Deviation (SD):** **0.00462** **0.03**

**Total Samples:** **50** **50**

**Total Passing Criterion:** **50** **50**

**Total Failing Criterion:** **0** **0**

**95%** **confidence Interval (Min/Max)** **3.272/3.275** **3.184/3.201**

**Total Samples Outside Range:** **2** **6**

**OCV >or= 3.200**

**CCV >or= 2.700 @ 1421 Ohms for 5 Seconds.**

**CUMULATIVE TABLE**

|  |  |  |  |
| --- | --- | --- | --- |
| **All Sample OCV** | | **All Sample CCV** | |
| Voltage Range | Samples | Voltage Range | Samples |
| 3.282-3.279 | 5 | 3.214-3.192 | 39 |
| 3.279-3.276 | 5 | 3.192-3.170 | 6 |
| 3.276-3.273 | 19 | 3.170-3.148 | 2 |
| 3.273-3.270 | 12 | 3.148-3.126 | 2 |
| 3.270-3.267 | 6 | 3.126-3.104 | 0 |
| 3.267-3.264 | 1 | 3.104-3.082 | 0 |
| 3.264-3.261 | 1 | 3.082-3.060 | 0 |
| 3.261-3.258 | 0 | 3.060-3.038 | 0 |
| 3.258-3.255 | 1 | 3.038-3.016 | 1 |