**SCREENING REPORT**

**Test Number:** 14462C00  **Date:**2021-03-04

**Sample Name:** Renata CR2032REN

**Chemistry:** Li/MnO₂

**Voltage Statistic Table**

All samples OCV CCV

**Maximum:** **3.282** **3.214**

**Minimum:** **3.255** **3.018**

**Median:** **3.274** **3.200**

**Mean (M):** **3.274** **3.193**

**Stander Deviation (SD):** **0.00462** **0.03**

**Total Samples:** **50** **50**

**Total Passing Criterion:** **50** **50**

**Total Failing Criterion:** **0** **0**

**95%** **confidence Interval**  3.272 / 3.275 3.184 / 3.201

**Outlier Min/Max** 3.266 / 3.282 3.175 / 3.224

**Total Outlier:** 2 6

**OCV > or =** 3.200**V**

**CCV > or =** 2.700 **@** 1421 Ohms for 5 Seconds.

**CUMULATIVE TABLE**

|  |  |  |  |
| --- | --- | --- | --- |
| **All Sample OCV** | | **All Sample CCV** | |
| Voltage Range | Samples | Voltage Range | Samples |
| 3.282-3.278 | 7 | 3.214-3.191 | 40 |
| 3.278-3.274 | 13 | 3.191-3.168 | 6 |
| 3.274-3.270 | 21 | 3.168-3.145 | 1 |
| 3.270-3.266 | 7 | 3.145-3.122 | 2 |
| 3.266-3.262 | 1 | 3.122-3.099 | 0 |
| 3.262-3.258 | 0 | 3.099-3.076 | 0 |
| 3.258-3.254 | 1 | 3.076-3.053 | 0 |
| 3.254-3.250 | 0 | 3.053-3.030 | 0 |
|  |  | 3.030-3.007 | 1 |