**SCREEING REPORT**

**Test Number:** 14575A00  **Date:**2020-01-31

**Sample Name:** Duracell MX2500

**Chemistry:** Zn/MnO2

**Pre-Tab** **Voltage Statistic Table**

All samples OCV

**Maximum:** **1.577**

**Minimum:** **1.554**

**Median:** **1.573**

**Mean (M):** **1.572**

**Stander Deviation (SD):** **0.00394**

**Total Samples:** **50**

**Total Passing Criterion:** **42**

**Total Failing Criterion:** **8**

**95% confidence Interval (Min/Max)** **1.570/1.573**

**Total Samples Outside Range:** **3**

**OCV >or= 1.570**

**CUMULATIVE TABLE**

|  |  |
| --- | --- |
| **All Sample OCV** | |
| Voltage Range | Samples |
| 1.577-1.574 | 6 |
| 1.574-1.571 | 25 |
| 1.571-1.568 | 13 |
| 1.568-1.565 | 2 |
| 1.565-1.562 | 2 |
| 1.562-1.559 | 1 |
| 1.559-1.556 | 0 |