**SCREENING REPORT**

**Test Number:** 14856-00  **Date:**2021-03-05

**Sample Name:** UHE-ER34615-H

**Chemistry:** Li/SOCl₂

**Profile Two** **Voltage Statistic Table**

All samples OCV CCV

**Maximum:** **3.682** **3.581**

**Minimum:** **3.667** **3.164**

**Median:** **3.678** **3.517**

**Mean (M):** **3.678** **3.493**

**Stander Deviation (SD):** **0.0026** **0.07179**

**Total Samples:** **72** **72**

**Total Passing Criterion:** **72** **72**

**Total Failing Criterion:** **0** **0**

**95%** **confidence Interval**  3.677 / 3.678 3.476 / 3.510

**Outlier Min/Max** 3.672 / 3.685 3.377 / 3.627

**Total Outlier:** 3 7

**OCV > or =** 3.630**V**

**CCV > or =** 3.000V **@** 184 Ohms for 5 Seconds.

**CUMULATIVE TABLE**

|  |  |  |  |
| --- | --- | --- | --- |
| **All Sample OCV** | | **All Sample CCV** | |
| Voltage Range | Samples | Voltage Range | Samples |
| 3.682-3.679 | 19 | 3.581-3.538 | 14 |
| 3.679-3.676 | 36 | 3.538-3.495 | 28 |
| 3.676-3.673 | 14 | 3.495-3.452 | 20 |
| 3.673-3.670 | 1 | 3.452-3.409 | 1 |
| 3.670-3.667 | 1 | 3.409-3.366 | 4 |
| 3.667-3.664 | 1 | 3.366-3.323 | 3 |
| 3.664-3.661 | 0 | 3.323-3.280 | 1 |
|  |  | 3.280-3.237 | 0 |
|  |  | 3.237-3.194 | 0 |
|  |  | 3.194-3.151 | 1 |