**SCREEING REPORT**

**Test Number:** 32186A  **Date:**2019-12-05

**Sample Name:** Maccor BT920349-001

**Chemistry:** Peter asdasd

**Post-Tab** **Voltage Statistic Table**

All samples OCV CCV

**Maximum:** **1.858** **1.558**

**Minimum:** **1.700** **1.470**

**Median:** **1.832** **1.532**

**Mean (M):** **1.827** **1.528**

**Stander Deviation (SD):** **0.01877** **0.01485**

**Total Samples:** **99** **99**

**Total Passing Criterion:** **99** **99**

**Total Failing Criterion:** **0** **0**

**95%** **confidence Interval (Min/Max)** **1.823/1.831** **1.525/1.531**

**Total Samples Outside Range:** **5** **5**

**OCV >or= 1.515**

**CCV >or= 1.300 @ 100 mA for 2 Seconds.**

**CUMULATIVE TABLE**

|  |  |  |  |
| --- | --- | --- | --- |
| **All Sample OCV** | | **All Sample CCV** | |
| Voltage Range | Samples | Voltage Range | Samples |
| 1.858-1.842 | 5 | 1.558-1.549 | 1 |
| 1.842-1.826 | 57 | 1.549-1.540 | 10 |
| 1.826-1.810 | 31 | 1.540-1.531 | 39 |
| 1.810-1.794 | 2 | 1.531-1.522 | 19 |
| 1.794-1.778 | 1 | 1.522-1.513 | 22 |
| 1.778-1.762 | 2 | 1.513-1.504 | 3 |
| 1.762-1.746 | 0 | 1.504-1.495 | 1 |
| 1.746-1.730 | 0 | 1.495-1.486 | 0 |
| 1.730-1.714 | 0 | 1.486-1.477 | 1 |
| 1.714-1.698 | 1 | 1.477-1.468 | 3 |