**SCREEING REPORT**

**Test Number:** 14665B01  **Date:**2020-01-06

**Sample Name:** Sony/Murata VTC6-18650

**Chemistry:** Li-Ion

**Section Two** **Voltage Statistic Table**

All samples OCV CCV

**Maximum:** **1.816** **1.811**

**Minimum:** **1.527** **1.494**

**Median:** **1.793** **1.789**

**Mean (M):** **1.732** **1.722**

**Stander Deviation (SD):** **0.12475** **0.13455**

**Total Samples:** **7** **7**

**Total Passing Criterion:** **5** **5**

**Total Failing Criterion:** **2** **2**

**95%** **confidence Interval (Min/Max)** **1.616/1.847** **1.598/1.846**

**Total Samples Outside Range:** **0** **0**

**OCV >or= 1.700**

**CCV >or= 1.600 @ 200 Ohms for 5 Seconds.**

**CUMULATIVE TABLE**

|  |  |  |  |
| --- | --- | --- | --- |
| **All Sample OCV** | | **All Sample CCV** | |
| Voltage Range | Samples | Voltage Range | Samples |
| 1.816-1.720 | 5 | 1.811-1.705 | 5 |
| 1.720-1.624 | 0 | 1.705-1.599 | 0 |
| 1.624-1.528 | 1 | 1.599-1.493 | 2 |